## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024‒05–29
Notes: Hello and welcome!
My name is Gottfrid Olsson and this master’s thesis is about electrochemical deposition of lithium on copper.

## Slide 2: PLAN: 25 minute presentation
// J och V_hold I text vid figurer
//deponerat Li på SEM-bilderna

## Slide 3: Batteries!
//Opening: How many here have either a smartphone, a laptop, or a smartwatch?
Cool, then you are already fans of batteries, and you likely own at least one lithium-ion battery – a very common battery type
Say, would you like your device to be smaller, lighter, and have a longer battery life? Of course you would!
It’s easy, look: replace this graphite with Li and the cell increases its energy per weight and doubles the energy per volume – very nice!
A) Let’s use this battery. Oh… what’s happening? Without the graphite, Li gets deposited on the surface. The Li grows unevenly, and oh no – look – it reached the other side of the cell! It’s a short-circuit, and [thermal runaway] *BOOM* [cell explosion] Yikes. Not good. Uneven deposition seems to be a problem.
B) However, there are several problems with such a lithium-metal battery.
//Kanske börja lite roligare som “opening:” beskriver, men sen ta (B) istället för (A).
Notes: Batteries
Lithium-ion battery very common type; you probably have it!
Lighter and smaller by replacing graphite in LIB with Li-metal
But problems!

## Slide 4: Batteries!
Notes: How many here have either a smartphone, a laptop, or a smartwatch? [raise my hand]
Cool, then you are already fans of batteries, and you likely own at least one lithium-ion battery – a very common battery type …

## Slide 5: Batteries!
Notes: It looks like this. [short pause]
Say, would you like your smartphone, laptop, or smartwatch to be smaller or lighter? Of course you would!
Well it’s easy, let’s replace the graphite with Li, …

## Slide 6: Batteries!
Notes: And violá!
We have a lithium-metal battery.
This change can …

## Slide 7: Batteries!
Notes: increase the specific energy and double the energy density of the cell.
This would not only make your laptop easier to carry, but would benefit for example electrical vehicles where the size and weight of today’s batteries are an obstacle.
Sounds too good to be true, right? =D
Yeah there are some problems, because the Li here can become uneven …
At the pack level:
* Li-ion cell: 150 Wh/kg, 250 Wh/L
Li-metal cell: 250 Wh/kg, 750 Wh/L
(http://large.stanford.edu/courses/2020/ph240/kim1/)

## Slide 8: Non-uniform deposition problems
Notes: Say we have a new cell which we charge and discharge: this means Li moves back and forth [point].

## Slide 9: Non-uniform deposition problems
Notes: Li can get deposited on the surface more in some places than others…

## Slide 10: Non-uniform deposition problems
Notes: Those places can then grow further…

## Slide 11: Non-uniform deposition problems
Notes: And more until, in the worst case…

## Slide 12: Non-uniform deposition problems
Notes: This grows until it reaches the other side and short circuits the cell. This can lead to an explosion, and is a safety risk.

## Slide 13: Non-uniform deposition problems
Notes: Short circuit is one of the problems caused by non-uniform deposition.
This green stuff is called the solid electrolyte interphase – SEI.
For low voltage, the electrolyte is broken down and reacts with Li to form this SEI layer.
It is generally good because it stops other reactions, but …if the SEI covers pieces of Li, they become electronically isolated and ‘’dead’’ as it can no longer contribute to the battery charge.
Also, the difference in volume between the deposited and the pristine Li induces mechanical stress, which can crack the SEI which then reforms, consuming more Li.
In short, non-uniform deposition is a safety risk [short circuit], and lowers the performance of the battery [dead and volume change].

## Slide 14: Non-uniform deposition problems
Notes: Short circuit is one of the problems caused by non-uniform deposition.
This green stuff is called the solid electrolyte interphase – SEI.
For low voltage, the electrolyte is broken down and reacts with Li to form this SEI layer.
It is generally good because it stops other reactions, but …if the SEI covers pieces of Li, they become electronically isolated and ‘’dead’’ as it can no longer contribute to the battery charge.
Also, the difference in volume between the deposited and the pristine Li induces mechanical stress, which can crack the SEI which then reforms, consuming more Li.
In short, non-uniform deposition is a safety risk [short circuit], and lowers the performance of the battery [dead and volume change].

## Slide 15: Non-uniform deposition problems
Notes: Short circuit is one of the problems caused by non-uniform deposition.
This green stuff is called the solid electrolyte interphase – SEI.
For low voltage, the electrolyte is broken down and reacts with Li to form this SEI layer.
It is generally good because it stops other reactions, but …if the SEI covers pieces of Li, they become electronically isolated and ‘’dead’’ as it can no longer contribute to the battery charge.
Also, the difference in volume between the deposited and the pristine Li induces mechanical stress, which can crack the SEI which then reforms, consuming more Li.
In short, non-uniform deposition is a safety risk [short circuit], and lowers the performance of the battery [dead and volume change].

## Slide 16: Purpose of this thesis
Nucleation – first step in the deposition
Pressure, current, passivation
Electrochemical measurements and scanning electron microscopy (SEM)
//figurer för dessa
Notes: To avoid non-uniform deposition, the first step in deposition of Li – nucleation, must be well understood.
The purpose then is to investigate how pressure, current and passivation (the SEI-layer) influences the nucleation.
By understanding nucleation better, ways of inducing more uniform – good – deposition can be found.
I have used electrochemical measurements and also scanning electron microscopy (SEM) to image the Li.

## Slide 17: Deposition in a Li/Cu cell
Notes: How does deposition work?
Here is a schematic of a Li/Cu cell.
Voltage difference  electrical fields  force on positive charges, Li+.
Electrons are released [point] and then recombines with the Li [point].

## Slide 18: Deposition in a Li/Cu cell
Notes: As more charge is passed (measure current, the electrons), more and more Li is deposited.

## Slide 19: Deposition in a Li/Cu cell
Notes: We identify two stages: nucleation and growth.
Nucleation is the first part and the focus of this thesis.

## Slide 20: Deposition in a Li/Cu cell
Notes: Let’s look at how the cell voltage varies with charge passed during deposition.

## Slide 21: Deposition in a Li/Cu cell
Notes: There is first a sharp drop in potential, reaching a lowest value of eta – this we will call the overpotential of nucleation.
At this point of the curve, nucleation occurs.

## Slide 22: Deposition in a Li/Cu cell
Notes: Then, the voltage goes up and the nuclei grow.

## Slide 23: Deposition in a Li/Cu cell
Notes: And they continue to grow as more charge get passed.
So, the focus is on the nucleation part.
What is nucleation?

## Slide 24: Nucleation
Notes: Nucleation is the first step in forming a new phase within a substance.
In our case, imagine Li-ions in a solution – a liquid.

## Slide 25: Nucleation
Notes: A Li+ ion can take up an electron and …

## Slide 26: Nucleation
Notes: Become a Li atom on the Cu surface.

## Slide 27: Nucleation
Notes: If several Li atoms come together …

## Slide 28: Nucleation
Notes: A small cluster is formed.

## Slide 29: Nucleation
Notes: As more Li+ ions get reduced and adsorbs to the cluster…

## Slide 30: Nucleation
Notes: A nucleus is formed.
This sequence, the formation of the new SOLID phase from the LIQUID, is called nucleation.
It is useful to model this with nucleation theory.

## Slide 31: Nucleation theory
Notes: Nucleation is modelled by looking at the change in Gibbs free energy as function of radius (assuming a spherical nucleus).

## Slide 32: Nucleation theory
Notes: To form the new phase, there is a cost for creating surface area.
It grows as r-squared.

## Slide 33: Nucleation theory
Notes: At the same time, there is a gain in energy from creating bulk. Scaling as minus r-cubed.

## Slide 34: Nucleation theory
Notes: The sum of these, DeltaG, is the change in Gibs free energy for creating a nucleus of a certain size r.
It costs energy to build a nucleus, up until this point…

## Slide 35: Nucleation theory
Notes: This is the critical radius, where the nucleus start to grow spontaneously as this lowers the overall energy of the system.
Because for large r the bulk-term dominates.
But to get to that point, there is an energy barrier …

## Slide 36: Nucleation theory
Notes: Delta G_barrier, which needs to be overcome.

## Slide 37: Nucleation theory
Notes: We saw the effect of this barrier in the deposition curve, with the sharp drop in the voltage.
We need to put in energy for the Li to nucleate.

## Slide 38: Nucleation theory
Notes: Writing out the expression for DeltaG, one can show that the size of the nucleus r is inversely proportional to the overpotential eta, and that the number of nuclei per area N is proportional to the third power of the overpotential.

## Slide 39: Nucleation theory
Notes: Let’s see schematically what this means.

## Slide 40: Nucleation theory
Notes: For low overpotential: large and few nuclei.

## Slide 41: Nucleation theory
Notes: Increasing overpotential: smaller and more nuclei.

## Slide 42: Nucleation theory
Notes: Increasing overpotential: smaller and more nuclei.
In this way, the overpotential influences the nuclei distribution (size and nuclei per area).

## Slide 43: Specific scientific questions
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure distribution between the Li and Cu
Notes: Now, this thesis will focus on how the shape of the deposition curve, and how the distribution of the nuclei can be affected.

## Slide 44: Specific scientific questions
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure distribution between the Li and Cu
Notes: The shape will be investigated by looking at the degree of passivation of the Cu surface, and the current during deposition.

## Slide 45: Specific scientific questions
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure distribution between the Li and Cu
Notes: We will look at how the pressure affects the distribution of the nuclei.
The methods chosen are:
Electrochemical cycling (the deposition curve shown before)
Scanning electron microscope to image the Li nuclei
To have different pressures, we need different cell setups.

## Slide 46: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: First the coin cell, or C-cell.
The parts, add electrolyte to the separator and push them together …

## Slide 47: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: Then place it in this …

## Slide 48: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: And turn the handles, …

## Slide 49: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: Which closes the cell, and results in this.
Note that the spring now exerts a force in the cell, meaning there is pressure applied between the Li and Cu.
The other cell type is …

## Slide 50: The I-cell
Spring
Spacer
Nut
Sealing
rings
Metal rod
Main body
Li
Separator
Cu

## Slide 51: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu
Notes: The T-cell, because it has three metal rods attached to the main body in a T-shape.
Push parts together, …

## Slide 52: The T-cell
Notes: Before closing the cell, electrolyte is added …

## Slide 53: The T-cell
Notes: Through this gap made in the spacer.
As you can see in the zoom-in, the spacer keeps a distance between the Li and Cu – so no applied pressure between them!

## Slide 54: The T-cell
Notes: The assembled cell looks like this.

## Slide 55: Deposition protocol
//figure hooking up cells to the Biologic
Notes: Now we can make some cells and to get deposition, we must cycle the cells – run a deposition program or protocol on them.
Attach cables from the electrodes, Li and Cu, to the instrument.

## Slide 56: Deposition protocol
Notes: The first part of the protocol is the OCV – we check that the cell was assembled correctly by checking its voltage.

## Slide 57: Deposition protocol
Notes: Next is the important passivation – or SEI formation.
Here, we hold a constant and low voltage. This means that electrolyte is broken down and forms the SEI layer on the Cu.
The current, which is allowed to change freely, decreases fast and then slowly.

## Slide 58: Deposition protocol
Notes: The next step is the deposition.
A here a constant current is used, and the voltage is allowed to change freely.
This results in the deposition curve we saw earlier, with a sharp dip during the nucleation and then a flatter part during the growth.

## Slide 59: Deposition protocol
Notes: The protocol was set up to end the SEI formation once a low current I_SEIcutoff was reached.

## Slide 60: Deposition protocol
Notes: And the deposition occurred at current Ideposition.

## Slide 61: Deposition protocol
Notes: The ratio between these, sigma, was used to try to have the same ratio of side reactions during the deposition (side reactions are all reactions besides deposition), for different deposition currents.

## Slide 62: Passivation of the Cu surface
Notes: To investigate the passivation of the Cu surface before deposition, several T-cell were cycled

## Slide 63: Passivation of the Cu surface
At 1 mAh/cm2
Notes: First, the current versus time during the SEI formation by holding a constant low voltage.
T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50

## Slide 64: Passivation of the Cu surface
Notes: First, the current versus time during the SEI formation by holding a constant low voltage.
T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50, 2 hour for 0.05
After the passivation, Li was deposited at constant current

## Slide 65: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential

## Slide 66: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 67: Passivation of the Cu surface larger charge passed
Notes: (hidden) T-cell, 1 mAh/cm2

## Slide 68: Deposition current
Notes: Several C-cells were cycled to see the effects of the deposition current.

## Slide 69: Deposition current
Notes: Increasing current, J, results in a higher overpotential.
However, with the same sigma, the nucleation peak disappears for larger currents.
We just saw that the deposition peak is dependent on sigma, so what would happen if we passivated the surface more?

## Slide 70: Deposition current with more passivation
Notes: Now the deposition peak becomes visible for larger currents.
As discussed, the more pronounced deposition peak indicates more instantaneous nucleation.
Thus, the absolute passivation, I_SEI-cutoff, influences the nucleation process.

## Slide 71: Deposition current with more passivation larger charge passed
Notes: The cells reach more or less the same potential at larger charge passed, indicating either that:
1. The surface gets passivated during the beginning of the deposition.
2. Or, that the growth is not as sensitive to the side reactions as the nucleation is.

## Slide 72: Pressure effects
Notes: To investigate the effect of pressure, a C-cell was first cycled

## Slide 73: Pressure effects
Notes: Photograph Li on Cu
uneven deposition from the annulus: little to no Li in the middle, more for larger radii
Photograph: 500 muAh/cm2
SEM-images: 25 muAh/cm2 at 1mA/cm2

## Slide 74: Pressure effects
Notes: SEM-images, overlain: matched the features on the images with each other to give a view of a larger area

## Slide 75: Pressure effects
Notes: Zoom in: see small Lithium nuclei

## Slide 76: Pressure effects
Notes: Moving down, slightly larger nuclei

## Slide 77: Pressure effects
Notes: Here even larger nuclei
Thus, for various radial positions we see different morphologies of Li: from small crystalline particles to larger ‘’islands’’

## Slide 78: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm
Notes: The typical size (diameter) of the nuclei goes from 1 here, 2 to 3, and then larger than 4.

## Slide 79: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm
Notes: Nuclei per area decreases while the nuclei size increases

## Slide 80: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm
Notes: These relations should be familiar

## Slide 81: Pressure effects
Notes: So, the distribution changes radially. How about the along the edge of the deposition?

## Slide 82: Pressure effects
Notes: SEM images for different angles around the edge of the deposition.
Photograph: 500 muAh/cm2
SEM-images: 50 muAh/cm2 at 1mA/cm2

## Slide 83: Pressure effects
Notes: Zoom in: see some particles, and bush-like growth

## Slide 84: Pressure effects
Notes: Here it’s mostly round particles

## Slide 85: Pressure effects
Notes: Down here: overwhelmingly bush-like growth.
Yes, the deposition changes also with the angle along the deposited annulus

## Slide 86: Pressure effects
Wave spring
Notes: The reason is probably the wave spring used in the C-cell.
A study found that the wave spring induces uneven pressure in the cell, with low pressure in the middle and higher pressure for larger radii.
Exactly as the annulus of deposited Li shows.
Photograph shows that the wave spring pushes down at some points, which could explain the angular variation.
For example, more pressure here and here (bush-like growth) compared to here (mostly particles)

## Slide 87: Pressure effects
Notes: To verify that even pressure makes even deposition, a T-cell was cycled and measured in SEM

## Slide 88: Pressure effects
Notes: SEM images as before, over the same distance the Li distribution seems more or less the same – at least much more even than in the C-cell

## Slide 89: Pressure effects
Notes: Zoom-in shows that the morphology is small crystalline particles, with longer and thinner needle-like growths.
While ‘’islands’’ are not observed in the T-cell, this needle-like growth might evolve into the bush-like growth we saw in the C-cell.

## Slide 90: Conclusions
More instantaneous nucleation can be induced by passivating the surface more before deposition.
To drive a large current during nucleation, a larger overpotential is necessary. This should influence the nuclei distribution.
Uniform pressure between the electrodes is essential to achieve uniform deposition in lithium-metal batteries.
Notes: Larger J  larger overpotential ( smaller r, larger N)
More passivation  larger overpotential ( smaller r, larger N)

## Slide 91: Conclusions
1) More instantaneous nucleation can be induced by passivating the surface more before deposition.

## Slide 92: Conclusions
2) To drive a larger current, a larger overpotential is necessary. This should result in smaller nuclei with larger areal density.

## Slide 93: Conclusions
3) Uniform pressure between the electrodes is essential to achieve uniform deposition in Li-metal batteries.

## Slide 94
Thank you for listening!

## Slide 95
//Lägg in fler plots här efter på större charge och andra figurer som Isak kanske kommenterar

## Slide 96: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024‒05‒29