## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024‒05–29
Notes: Hello and welcome!
My name is Gottfrid Olsson and this master’s thesis is about electrochemical deposition of lithium on copper.

## Slide 2: PLAN: 25 minute presentation
// J och V_hold I text vid figurer
//deponerat Li på SEM-bilderna

## Slide 3: Batteries!
//Opening: How many here have either a smartphone, a laptop, or a smartwatch?
Cool, then you are already fans of batteries, and you likely own at least one lithium-ion battery – a very common battery type
Say, would you like your device to be smaller, lighter, and have a longer battery life? Of course you would!
It’s easy, look: replace this graphite with Li and the cell increases its energy per weight and doubles the energy per volume – very nice!
A) Let’s use this battery. Oh… what’s happening? Without the graphite, Li gets deposited on the surface. The Li grows unevenly, and oh no – look – it reached the other side of the cell! It’s a short-circuit, and [thermal runaway] *BOOM* [cell explosion] Yikes. Not good. Uneven deposition seems to be a problem.
B) However, there are several problems with such a lithium-metal battery.
//Kanske börja lite roligare som “opening:” beskriver, men sen ta (B) istället för (A).
Notes: Batteries
Lithium-ion battery very common type; you probably have it!
Lighter and smaller by replacing graphite in LIB with Li-metal
But problems!

## Slide 4: Batteries!
Notes: How many here have either a smartphone, a laptop, or an electric car? [raise my hand]
Cool, then you are using batteries every day, and you likely own at least one lithium-ion battery – a very common battery type …

## Slide 5: Batteries!
Notes: These are the parts. [short pause]
If we replace the graphite with Li …

## Slide 6: Batteries!
Notes: We get a lithium-metal battery.
This change from graphite to lithium can …

## Slide 7: Batteries!
Notes: Drastically increase the energy per weight and doubles the energy per volume of the cell.
This would not only make your laptop easier to carry, but would benefit for example electrical vehicles where the size and weight of today’s batteries are an obstacle.
In the Li-ion cell, Li moves between the metal oxide and into the graphite.
Having removed the graphite, the Li must instead deposit on the surface.
This unfortunately leads to some problems.
At the pack level:
* Li-ion cell: 150 Wh/kg, 250 Wh/L
Li-metal cell: 250 Wh/kg, 750 Wh/L
(http://large.stanford.edu/courses/2020/ph240/kim1/)

## Slide 8: Non-uniform deposition problems
Notes: Say we have a new cell which we charge and discharge many times: this means Li moves up during discharging [point], and back down during charging [point].

## Slide 9: Non-uniform deposition problems
Notes: Li can over time get deposited on the surface more in some places than others…

## Slide 10: Non-uniform deposition problems
Notes: Those places can then grow further…

## Slide 11: Non-uniform deposition problems
Notes: And even more until, in the worst case…

## Slide 12: Non-uniform deposition problems
Notes: It reaches the other side and short circuits the cell. This can lead to an explosion, and is a major safety risk.

## Slide 13: Non-uniform deposition problems
Notes: Short circuit is one of the problems caused by non-uniform deposition.
Other problems has to do with this this green stuff called the solid electrolyte interphase – SEI.
For low voltage, the electrolyte is chemically broken down and reacts with the Li, forming this SEI layer.
It is generally good because it passivates the surface – preventing other reactions from occurring.
But …

## Slide 14: Non-uniform deposition problems
Notes: if the SEI covers a piece of Li, it becomes electronically isolated and ‘’dead’’ as it can no longer contribute to the battery charge.
This lowers the lifetime of the battery.

## Slide 15: Non-uniform deposition problems
Notes: Also, the difference in volume between the deposited and the pristine Li induces mechanical stress, which can crack the SEI.
This exposes fresh Li to the electrolyte, and more SEI is formed which consumes Li.
In short, non-uniform deposition is a safety risk [short circuit], and lowers the performance of the battery by creating dead Li [dead Li] and extra SEI.
So this is bad, how can it be avoided?

## Slide 16: Purpose of this thesis
Notes: To avoid non-uniform deposition, the first step – nucleation, must be well understood. …

## Slide 17: Purpose of this thesis
Investigate the nucleation – the first step in deposition.
Notes: By understanding nucleation better, ways of achieving more uniform deposition can be found.
I have used …

## Slide 18: Purpose of this thesis
Investigate the nucleation – the first step in deposition.
Electrochemical measurements and scanning electron microscope.
Notes: To investigate this I’ve done electrochemical measurements, and taken scanning electron microscope (SEM) images of Li on Cu.
How does deposition work?

## Slide 19: Deposition in a Li/Cu cell
Notes: Here is a schematic of a Li/Cu cell.
Voltage difference  electrical field  excerts a force on positive charges, Li-ions.
Li atoms here can release their electrons [point].
The electrons moves along the circuit while the Li-ions moves toward the Cu.
Li-ions can recombine with electrons to form Li on the surface [point].

## Slide 20: Deposition in a Li/Cu cell
Notes: As more charge is passed – measured by the current in the circuit – more and more Li is deposited.

## Slide 21: Deposition in a Li/Cu cell
Notes: We identify two stages: nucleation in the beginning and then growth.

## Slide 22: Deposition in a Li/Cu cell
Notes: Let’s look at how the cell voltage varies with charge passed during deposition.

## Slide 23: Deposition in a Li/Cu cell
Notes: There is first a sharp drop in potential, reaching a lowest value of eta – this we will call the overpotential of nucleation.
Overpotential is how “deep” this peak is.
At this point of the curve, nucleation occurs.

## Slide 24: Deposition in a Li/Cu cell
Notes: Then, the voltage goes up and the nuclei grow.

## Slide 25: Deposition in a Li/Cu cell
Notes: And they continue to grow as more charge get passed.
So, the focus of this thesis is on the nucleation [point].
What is nucleation?

## Slide 26: Nucleation
Notes: Nucleation is the first step in forming a new phase within a substance.

## Slide 27: Nucleation
Notes: In our case, imagine Li-ions in a solution – a liquid.

## Slide 28: Nucleation
Notes: A Li+ ion can take up an electron and …

## Slide 29: Nucleation
Notes: Become a Li atom on the Cu surface.

## Slide 30: Nucleation
Notes: If several Li atoms come together …

## Slide 31: Nucleation
Notes: A small cluster is formed.

## Slide 32: Nucleation
Notes: As more Li gets added to the cluster…

## Slide 33: Nucleation
Notes: Eventually a nucleus is formed.
This formation of the new SOLID phase from the LIQUID, is called nucleation.
It is useful to model this with theory.

## Slide 34: Nucleation theory
Notes: Nucleation is modelled by looking at the change in Gibbs free energy of the system as function of nucleus radius.
Here, we area assuming a spherical nucleus.

## Slide 35: Nucleation theory
Notes: To form the new phase, there is a cost for creating surface area.
It grows as r2.

## Slide 36: Nucleation theory
Notes: At the same time, there is a gain in energy from creating bulk, scaling as –r3.
The sum of these …

## Slide 37: Nucleation theory
Notes: DeltaG, is the change in Gibs free energy for creating a nucleus of a certain size r.
It costs energy to build a nucleus, up until this point…

## Slide 38: Nucleation theory
Notes: This is the critical radius, where the nucleus start to grow spontaneously as this lowers the overall energy of the system.
But to get to that point, there is an energy barrier …

## Slide 39: Nucleation theory
Notes: Delta G_barrier, which needs to be overcome.
And we saw the effect of this barrier…

## Slide 40: Nucleation theory
Notes: in the deposition curve, with the sharp drop in the voltage.
This overpotential is energy we put in to drive the nucleation.

## Slide 41: Nucleation theory
Notes: From nucleation theory, one can show that the size of the nucleus r is inversely proportional to the overpotential eta, and that the number of nuclei per area N is proportional to the third power of the overpotential.
What does this mean?

## Slide 42: Nucleation theory
Notes: This means that…

## Slide 43: Nucleation theory
Notes: For low overpotential: large and few nuclei.

## Slide 44: Nucleation theory
Notes: For increasing overpotential…

## Slide 45: Nucleation theory
Notes: smaller nuclei but more per area.
Thus, the overpotential influences the size and number of nuclei.
One can imagine that this [point] leads to more even deposition compared to this [point].

## Slide 46: Scientific questions in this thesis
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure distribution between the Li and Cu
Notes: This thesis will more specifically focus on how the shape of the deposition curve, and how the distribution of the nuclei can be affected.

## Slide 47: Scientific questions in this thesis
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure distribution between the Li and Cu
Notes: The shape will be investigated by looking at the degree of passivation of the Cu surface, and the current during deposition.

## Slide 48: Scientific questions in this thesis
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
 Electrochemical measurements
Notes: For this, I’ve taken electrochemical measurements.

## Slide 49: Scientific questions in this thesis
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure between the Li and Cu
 Electrochemical measurements
Notes: We will look at how the pressure between the Li and Cu affects the distribution of the nuclei.

## Slide 50: Scientific questions in this thesis
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Distribution of the nuclei
  Pressure between the Li and Cu
 Image Li nuclei using SEM
 Electrochemical measurements
Notes: For this, I’ve imaged Li nuclei using the SEM.
To have different pressures, we need different cell setups.

## Slide 51: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: First is the coin cell, or C-cell.
Note the parts: Li and Cu, the separator keeping them from touching, and also the spring.
During assembly, electrolyte is added to the separator and the parts pushed together …

## Slide 52: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: Then place this in the machine …

## Slide 53: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: and turn the handles [spin finger in circle]…

## Slide 54: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can
Notes: This closes the cell by folding in the edges, and results in this.
Note that the spring now exerts a force in the cell, meaning there is pressure applied between the Li and Cu.
The other cell type, without pressure, is …

## Slide 55: The I-cell
Spring
Spacer
Nut
Sealing
rings
Metal rod
Main body
Li
Separator
Cu

## Slide 56: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu
Notes: The T-cell, “T” because it has three metal rods attached to the main body in a T-shape. [pause]
Push the parts together, …

## Slide 57: The T-cell
Notes: And before putting in the last metal rod, electrolyte is added …

## Slide 58: The T-cell
Notes: Through this gap made in the spacer you can see in the zoom-in.
The spacer keeps a distance between the Li and Cu – so there is no applied pressure between them.

## Slide 59: The T-cell
Notes: The assembled cell looks like this.
Now we can make C-cells and T-cells, and connect them to an instrument that controls and measures voltage and current.
To get deposition, we must run a deposition protocol …

## Slide 60: Deposition protocol
Notes: This protocol is shown as the voltage and current as function of time.

## Slide 61: Deposition protocol
Notes: The first part of the protocol is the open circuit voltage.
We check that the voltage of the cell is good, meaning it was assembled correctly.

## Slide 62: Deposition protocol
Notes: Next is the important passivation – or SEI formation.
Here, we hold a constant and low voltage.
The electrolyte is broken down and forms the SEI layer on the Cu.
The current, which is allowed to change freely, decreases fast and then slowly.

## Slide 63: Deposition protocol
Notes: The next step is the deposition.
A constant current is used, and the voltage is allowed to change freely.
This results in the deposition curve we saw earlier.

## Slide 64: Deposition protocol
Notes: The protocol was set up to end the SEI formation once a low cutoff current was reached.
During the low voltage hold, side reactions occur in the cell, including the SEI formation.
As the SEI layer grows in thickness, the side reactions decrease which we can see from the decrease in current.
This is what we mean by “passivating the surface”.

## Slide 65: Deposition protocol
Notes: The deposition occurred at current I_deposition.
Now my specific research questions becomes more clear.
I have investigated how:
1) the deposition curve [point] is influenced by different cutoff currents [point], …

## Slide 66: Deposition protocol
Notes: here…

## Slide 67: Deposition protocol
Notes: Here…

## Slide 68: Deposition protocol
Notes: Or here.
And 2) how the deposition curve [point] varies with different deposition currents [point]

## Slide 69: Deposition protocol
Notes: First, we look at different cutoff currents.

## Slide 70: Passivation of the Cu surface
Notes: Several T-cell were cycled.

## Slide 71: Passivation of the Cu surface
Notes: Here we see the current versus time during the SEI formation by holding a constant low voltage.
I have stopped the SEI formation for here for one cell, here for another, and here for another.
After the passivation, Li was deposited at constant current

## Slide 72: Passivation of the Cu surface
Ideposition = 196 µA
Jdeposition = 1 mA/cm2
Notes: For large cutoff current: no obvious nucleation; side reactions large enough to drive current without need for nucleation in the beginning
For more passivation, smaller cutoff current  see clearer deposition peak, at larger overpotential
More passivation means less side reactions.
If there are no side reactions then only deposition of Li can provide the current,
 it is necessary to nucleate a lot in the beginning, which happens if the overpotential is large
Thus, more passivation leads to more instantaneous nucleation, where more or less all nuclei form at the start and then they all grow

## Slide 73: Passivation of the Cu surface larger charge passed
Ideposition = 196 µA
Jdeposition = 1 mA/cm2
Notes: (hidden) T-cell, 1 mAh/cm2

## Slide 74: Deposition protocol
Notes: Now, let’s look at how different currents during deposition influences the deposition curve.

## Slide 75: Deposition current
Notes: C-cells were cycled with three different currents.

## Slide 76: Deposition current
Notes: One current, a larger one, and an even larger current.
See: larger current  results in a higher overpotential.
And higher overpotential should according to theory…
{J=1, 5, 10 mA/cm2}

## Slide 77: Deposition current
Notes: Result in smaller but more nuclei.
In this case, ratio of the cutoff and deposition current are the same.
And the nucleation peak disappears for larger currents.
We just saw that this [point] peak is dependent on the cutoff current, so what happens if we passivate the surface more?

## Slide 78: Deposition current with more passivation
Notes: Here are the same three currents, with more passivation.
Now the deposition peak becomes visible for larger currents.
As discussed, the more pronounced deposition peak, with larger overpotential, indicates more instantaneous nucleation.
Thus, the current used should influence r and N, and the degree of passivation influences the nucleation process.
{J=1, 5, 10 mA/cm2}

## Slide 79: Deposition current with more passivation larger charge passed
Notes: The cells reach more or less the same potential at larger charge passed, indicating either that:
1. The surface gets passivated during the beginning of the deposition.
2. Or, that the growth is not as sensitive to the side reactions as the nucleation is.

## Slide 80: Pressure effects
Notes: To investigate the effect of pressure, a C-cell was first cycled

## Slide 81: Pressure effects
Notes: Photograph deposited Li on Cu:
We see uneven deposition from the annulus: little to no Li in the middle, but more for larger radii
Photograph: 500 muAh/cm2
SEM-images: 25 muAh/cm2 at 1mA/cm2

## Slide 82: Pressure effects
25 µAh/cm2
Notes: SEM-images were taken for different radii.
Here I’ve matched the features on the images with each other to give a view of a larger area.
Zooming in…

## Slide 83: Pressure effects
25 µAh/cm2
Notes: we see small Li nuclei.

## Slide 84: Pressure effects
25 µAh/cm2
Notes: Moving down, see slightly larger nuclei.

## Slide 85: Pressure effects
25 µAh/cm2
Notes: Here even larger nuclei.
Thus, for various radial positions [point] we see different morphologies of Li: from small crystalline particles to larger ‘’islands’’.

## Slide 86: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm
25 µAh/cm2
Notes: The typical size (diameter) of the nuclei goes from 1 micro meter here, 2 to 3, and then larger than 4.

## Slide 87: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm
25 µAh/cm2
Notes: Nuclei per area decreases while the nuclei size increases.

## Slide 88: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm
25 µAh/cm2
Notes: These relations should be familiar by now. ;)

## Slide 89: Pressure effects
Notes: So, the distribution changes radially. How about the along the edge of the deposition?

## Slide 90: Pressure effects
50 µAh/cm2
Notes: SEM images for different angles around the edge of the deposition.
Photograph: 500 muAh/cm2
SEM-images: 50 muAh/cm2 at 1mA/cm2

## Slide 91: Pressure effects
50 µAh/cm2
Notes: Zoom in: see some particles, and also bush-like growth

## Slide 92: Pressure effects
50 µAh/cm2
Notes: Here it’s mostly round particles

## Slide 93: Pressure effects
Notes: Down here: overwhelmingly bush-like growth.
Yes, the deposition changes also with the angle along the deposited annulus.

## Slide 94: Pressure effects
Wave spring
Notes: The reason is probably due to the wave spring used in the C-cell.
A study found that the wave spring induces uneven pressure in the cell, with low pressure in the middle and higher pressure for larger radii.
Exactly as the annulus of deposited Li shows – with little deposition for low pressure, and more deposition for high pressure.
Photograph shows that the wave spring pushes down at some points [point],
which could explain the angular variation with more deposition, bush-like growth, at those points.

## Slide 95: Pressure effects
Notes: We have seen that uneven pressure leads to uneven deposition.
Does even pressure make more even deposition?
To find that out, a T-cell was cycled.

## Slide 96: Pressure effects
300 µAh/cm2
Notes: SEM images as before, over the same distance as in the C-cell, the Li distribution is much more evenly distributed.

## Slide 97: Pressure effects
300 µAh/cm2
Notes: Zoom-in shows that the morphology is small crystalline particles, with longer and thinner needle-like growth.
While ‘’islands’’ were not observed in the T-cell, we can image that this needle-like growth might evolve into the bush-like growth we saw in the C-cell.
What have we learned? …

## Slide 98: Conclusions
1) More instantaneous nucleation can be induced by passivating the surface more before deposition.

## Slide 99: Conclusions
2) For larger currents, larger overpotential is seen. This should result in smaller nuclei with larger areal density.

## Slide 100: Conclusions
3) Uniform pressure between the electrodes is essential to achieve uniform deposition in Li-metal batteries.

## Slide 101
Thank you for listening!

## Slide 102
//Lägg in fler plots här efter på större charge och andra figurer som Isak kanske kommenterar

## Slide 103: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024‒05‒29