## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-29

## Slide 2: PLAN: 25 minute presentation
Introduction:
  Importance of batteries, improvements LMB>LIB (fig.), problems non-uniform growth (fig + in-depth), purpose of this thesis
Theory:
  Homogenous nucleation theory; main results (fig.), how does eta impact r and N (fig.)?
Methods:
  Cell assemblies (note importances; wave spring, no pressure); cycling protocol (fig.)
Results:
  passivation of Cu; J-dep.; pressure (C-cell and T-cell, r & angle dep. and morphology)
Conclusion: 2 min
  Passivation, J-dep. and pressure to achieve uniform deposition in LMBs
(Opposition and Questions from audience)

## Slide 3: Introduction
Batteries
Lithium-ion battery very common type; you probably have it!
Lighter and smaller by replacing graphite in LIB with Li-metal

## Slide 4: Batteries!
Opening: How many here have either a smartphone, a laptop, or a smartwatch?
Cool, then you are already fans of batteries, and you likely own at least one lithium-ion battery – a very common battery type
Say, would you like your device to be smaller, lighter, and have a longer battery life? Of course you would!
It’s easy, look: replace this graphite with Li and the cell increases its energy per weight and doubles the energy per volume – very nice!
Let’s use this battery. Oh… what’s happening? Without the graphite, Li gets deposited on the surface. The Li grows unevenly, and oh no – look – it reached the other side of the cell! It’s a short-circuit, and [thermal runaway] *BOOM* [cell explosion]
Yikes. Not good. Uneven deposition seems to be a problem.
There are in fact several problems.

## Slide 5: Batteries!
//LIB one of the most used batteries today
Looks like this.
If replace graphite with Li, increase specific energy and double the energy density
Would benefit e.g. electrical vehicles (extra range)
However, problems bcs. Li depos on surface! (n.s.)
600 Wh L–1 to 1200 Wh L–1
250 Wh kg–1 to 440 Wh kg–1

## Slide 6: Non-uniform deposition problems

## Slide 7: Non-uniform deposition problems

## Slide 8: Purpose of this thesis
To avoid non-uniform deposition, the first step in deposition of Li – nucleation, must be well understood.
Purpose: investigate how pressure, current, and passivation influences the nucleation.
Scanning electron microscopy (SEM) and electrochemical cycling.

## Slide 9: Deposition in a Li/Cu cell

## Slide 10: Deposition in a Li/Cu cell

## Slide 11: Deposition in a Li/Cu cell

## Slide 12: Deposition in a Li/Cu cell

## Slide 13: Deposition in a Li/Cu cell

## Slide 14: Deposition in a Li/Cu cell

## Slide 15: Nucleation
Notes: Li-ions in solution (liquid)  Li-metal (solid)

## Slide 16: Nucleation

## Slide 17: Nucleation

## Slide 18: Nucleation

## Slide 19: Nucleation

## Slide 20: Nucleation

## Slide 21: Nucleation

## Slide 22: Nucleation theory

## Slide 23: Nucleation theory

## Slide 24: Nucleation theory

## Slide 25: Nucleation theory

## Slide 26: Nucleation theory

## Slide 27: Nucleation theory

## Slide 28: Nucleation theory

## Slide 29: Nucleation theory

## Slide 30: Nucleation theory

## Slide 31: Nucleation theory

## Slide 32: Nucleation theory

## Slide 33: Specific scientific questions
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Size and distribution of the nuclei
  Pressure distribution between the Li and Cu
Notes: For different pressure, we need two different cell setups

## Slide 34: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 35: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 36: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 37: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 38: The I-cell
Spring
Spacer
Nut
Sealing
rings
Metal rod
Main body
Li
Separator
Cu

## Slide 39: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu

## Slide 40: The T-cell

## Slide 41: The T-cell

## Slide 42: Deposition protocol

## Slide 43: Deposition protocol

## Slide 44: Deposition protocol

## Slide 45: Deposition protocol:

## Slide 46: Passivation of the Cu surface
Notes: To investigate the passivation of the Cu surface before deposition, several T-cell were cycled

## Slide 47: Passivation of the Cu surface
Notes: First, the current versus time during the SEI formation by holding a constant low voltage.
T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50

## Slide 48: Passivation of the Cu surface
Notes: First, the current versus time during the SEI formation by holding a constant low voltage.
T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50, 2 hour for 0.05
After the passivation, Li was deposited at constant current

## Slide 49: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential

## Slide 50: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 51: Passivation of the Cu surface larger charge passed
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 52: Deposition current
Notes: Several C-cells were cycled to see the affects of the deposition current.

## Slide 53: Deposition current
Notes: Increasing current, J, results in a higher overpotential.
However, with the same sigma, the nucleation peak disappears for larger currents.
We just saw that the deposition peak is dependent on sigma, so what would happen if we passivated the surface more?

## Slide 54: Deposition current with more passivation
Notes: See, now the deposition peak becomes visible for larger currents.
As discussed, the sharper deposition peak indicates more instantaneous nucleation.
Thus, the absolute passivation seems to be important, I_SEI-cutoff, since we then do see the nucleation peak for all current

## Slide 55: Deposition current with more passivation larger charge passed

## Slide 56: Pressure effects
Notes: To investigate the effect of pressure, a C-cell was cycled

## Slide 57: Pressure effects
Notes: Photograph Li on Cu
* uneven deposition from the annulus: little to no Li in the middle, more for larger radii

## Slide 58: Pressure effects
Notes: SEM-images, overlain: matched the features on the images with each other

## Slide 59: Pressure effects
Notes: Zoom in: see small Lithium nuclei

## Slide 60: Pressure effects
Notes: Moving down, slightly larger nuclei

## Slide 61: Pressure effects
Notes: Here even larger nuclei
Thus, for various radial positions we see different morphologies of Li: from small crystalline particles to larger ‘’islands’’

## Slide 62: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm
Notes: The typical size (diameter) of the nuclei goes from 1 here, 2 to 3, and then larger than 4.

## Slide 63: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm
Notes: Nuclei per area decreases while the nuclei size increases

## Slide 64: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm
Notes: These relations should be familiar

## Slide 65: Pressure effects
Notes: So, the distribution changes radially. How about the along the edge of the deposition?

## Slide 66: Pressure effects
Notes: SEM images for different angles around the edge of the deposition

## Slide 67: Pressure effects
Notes: Zoom in: see some particles, and bush-like growth

## Slide 68: Pressure effects
Notes: Here it’s mostly round particles

## Slide 69: Pressure effects
Notes: Down here overwhelmingly bush-like growth.
Yes, the deposition changes also with the angle along the deposited annulus

## Slide 70: Pressure effects
Wave spring
Notes: The reason is probably the wave spring used in the C-cell.
A study found that the wave spring induces uneven pressure in the cell, with low pressure in the middle and higher pressure for larger radii.
Exactly as the annulus of deposited Li shows.
Photograph shows that the wave spring pushed down at some points, which could explain the angular variation

## Slide 71: Pressure effects
Notes: To verify that the pressure influences the deposition, a T-cell was cycled and measured in SEM

## Slide 72: Pressure effects
Notes: SEM images as before, over the same distance the Li distribution seems more or less the same – at least much more even than in the C-cell

## Slide 73: Pressure effects
Notes: Zoom in shows that the morphology is small crystalline particles, with longer and thinner needle-like growths.
While ‘’islands’’ are not observed in the T-cell, this needle-like growth might evolve into the bush-like growth we saw in the C-cell.

## Slide 74: Conclusions
More instantaneous or more progressive nucleation depends on the current ratio of the side reactions and the deposition (σ).
The nuclei distribution (r and N) is influenced by the current and the degree of passivation (both changes the nucleation peak η).
Uniform pressure between the electrodes is essential to achieve uniform deposition.

## Slide 75
Thank you for listening!

## Slide 76
//Lägg in fler plots här efter på större charge och andra figurer som Isak kanske kommenterar

## Slide 77: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-29