## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-21

## Slide 2: PLAN: 25 minute presentation
Introduction:
  Importance of batteries, improvements LMB>LIB (fig.), problems non-uniform growth (fig + in-depth), purpose of this thesis
Theory:
  Homogenous nucleation theory; main results (fig.), how does eta impact r and N (fig.)?
Methods:
  Cell assemblies (note importances; wave spring, no pressure); cycling protocol (fig.)
Results:
  passivation of Cu; J-dep.; pressure (C-cell and T-cell, r & angle dep. and morphology)
Conclusion: 2 min
  Passivation, J-dep. and pressure to achieve uniform deposition in LMBs
(Opposition and Questions from audience)

## Slide 3: Batteries!

## Slide 4: Non-uniform deposition problems

## Slide 5: Purpose of this thesis
Investigate pressure, current, passivation

## Slide 6: Nucleation theory

## Slide 7: Nucleation theory
r ∝ η −1
N ∝ η 3

## Slide 8: Nucleation theory
r ∝ η −1
N ∝ η 3

## Slide 9: Nucleation theory
r ∝ η −1
N ∝ η 3

## Slide 10: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 11: The I-cell
Spring
Spacer
Nut
Sealing rings
Metal rod
Main body
Li
Cu
Separator

## Slide 12: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu

## Slide 13: The T-cell

## Slide 14: Cycling protocol

## Slide 15: Cycling protocol

## Slide 16: Cycling protocol

## Slide 17: Passivation of the Cu surface
Notes: T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50, 2 hour for 0.05, over 25 hours for 0.01

## Slide 18: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 19: Different deposition currents

## Slide 20: Pressure effects

## Slide 21: Pressure effects

## Slide 22: Pressure effects

## Slide 23: Pressure effects

## Slide 24: Pressure effects

## Slide 25: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm

## Slide 26: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 27: Pressure effects

## Slide 28: Pressure effects

## Slide 29: Pressure effects

## Slide 30: Pressure effects

## Slide 31: Pressure effects

## Slide 32: Pressure effects

## Slide 33: Pressure effects

## Slide 34: Pressure effects

## Slide 35: Conclusions

## Slide 36: //
Tank for listen.

## Slide 37: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-21