## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-21

## Slide 2: PLAN: 25 minute presentation
Introduction:
  Importance of batteries, improvements LMB>LIB (fig.), problems non-uniform growth (fig + in-depth), purpose of this thesis
Theory:
  Homogenous nucleation theory; main results (fig.), how does eta impact r and N (fig.)?
Methods:
  Cell assemblies (note importances; wave spring, no pressure); cycling protocol (fig.)
Results:
  passivation of Cu; J-dep.; pressure (C-cell and T-cell, r & angle dep. and morphology)
Conclusion: 2 min
  Passivation, J-dep. and pressure to achieve uniform deposition in LMBs
(Opposition and Questions from audience)

## Slide 3: Batteries!

## Slide 4: Non-uniform deposition problems

## Slide 5: Purpose of this thesis
Investigate pressure, current, passivation

## Slide 6: Deposition in a Li/Cu cell

## Slide 7: Deposition in a Li/Cu cell

## Slide 8: Deposition in a Li/Cu cell

## Slide 9: Nucleation theory
//describe: nucleation here: form solid Li from a solution of Li+ (figure!)
Use thermodynamics to theoretically model this (next slide)

## Slide 10: Nucleation theory

## Slide 11: Nucleation theory

## Slide 12: Nucleation theory

## Slide 13: Nucleation theory

## Slide 14: Nucleation theory

## Slide 15: Nucleation theory

## Slide 16: Nucleation theory

## Slide 17: Nucleation theory

## Slide 18: Nucleation theory

## Slide 19: Nucleation theory

## Slide 20: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 21: The I-cell
Spring
Spacer
Nut
Sealing
rings
Metal rod
Main body
Li
Separator
Cu

## Slide 22: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu

## Slide 23: The T-cell

## Slide 24: The T-cell

## Slide 25: Cycling protocol

## Slide 26: Cycling protocol

## Slide 27: Cycling protocol

## Slide 28: Passivation of the Cu surface
Notes: T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50, 2 hour for 0.05, over 25 hours for 0.01

## Slide 29: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 30: Different deposition currents

## Slide 31: Pressure effects

## Slide 32: Pressure effects

## Slide 33: Pressure effects

## Slide 34: Pressure effects

## Slide 35: Pressure effects

## Slide 36: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm

## Slide 37: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 38: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 39: Pressure effects

## Slide 40: Pressure effects

## Slide 41: Pressure effects

## Slide 42: Pressure effects

## Slide 43: Pressure effects

## Slide 44: Pressure effects

## Slide 45: Pressure effects

## Slide 46: Pressure effects

## Slide 47: Pressure effects

## Slide 48: Pressure effects

## Slide 49: Conclusions

## Slide 50: //
Tank for listen.

## Slide 51: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-21