## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-29

## Slide 2: PLAN: 25 minute presentation
Introduction:
  Importance of batteries, improvements LMB>LIB (fig.), problems non-uniform growth (fig + in-depth), purpose of this thesis
Theory:
  Homogenous nucleation theory; main results (fig.), how does eta impact r and N (fig.)?
Methods:
  Cell assemblies (note importances; wave spring, no pressure); cycling protocol (fig.)
Results:
  passivation of Cu; J-dep.; pressure (C-cell and T-cell, r & angle dep. and morphology)
Conclusion: 2 min
  Passivation, J-dep. and pressure to achieve uniform deposition in LMBs
(Opposition and Questions from audience)

## Slide 3: Batteries!

## Slide 4: Batteries!
600 Wh L–1 to 1200 Wh L–1
250 Wh kg–1 to 440 Wh kg–1

## Slide 5: Non-uniform deposition problems

## Slide 6: Non-uniform deposition problems

## Slide 7: Purpose of this thesis
Investigate pressure, current, passivation

## Slide 8: Deposition in a Li/Cu cell

## Slide 9: Deposition in a Li/Cu cell

## Slide 10: Deposition in a Li/Cu cell

## Slide 11: Nucleation theory
//describe: nucleation here: form solid Li from a solution of Li+ (figure!)
Use thermodynamics to theoretically model this (next slide)

## Slide 12: Nucleation theory

## Slide 13: Nucleation theory

## Slide 14: Nucleation theory

## Slide 15: Nucleation theory

## Slide 16: Nucleation theory

## Slide 17: Nucleation theory

## Slide 18: Nucleation theory

## Slide 19: Nucleation theory

## Slide 20: Nucleation theory

## Slide 21: Nucleation theory

## Slide 22: Nucleation theory

## Slide 23: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 24: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 25: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 26: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 27: The I-cell
Spring
Spacer
Nut
Sealing
rings
Metal rod
Main body
Li
Separator
Cu

## Slide 28: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu

## Slide 29: The T-cell

## Slide 30: The T-cell

## Slide 31: Deposition protocol

## Slide 32: Deposition protocol

## Slide 33: Deposition protocol

## Slide 34: Passivation of the Cu surface
Notes: T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50, 2 hour for 0.05, over 25 hours for 0.01

## Slide 35: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 36: Passivation of the Cu surface larger charge passed
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 37: Deposition current

## Slide 38: Deposition current with more passivation

## Slide 39: Pressure effects

## Slide 40: Pressure effects

## Slide 41: Pressure effects

## Slide 42: Pressure effects

## Slide 43: Pressure effects

## Slide 44: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm

## Slide 45: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 46: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 47: Pressure effects

## Slide 48: Pressure effects

## Slide 49: Pressure effects

## Slide 50: Pressure effects

## Slide 51: Pressure effects

## Slide 52: Pressure effects

## Slide 53: Pressure effects

## Slide 54: Pressure effects

## Slide 55: Conclusions
To induce more instantaneous or more progressive nucleation, σ can be tuned.
The surface must be properly passivated, as it affects the nucleation peak and thus the nuclei distribution (r and N).
Uniform pressure between the electrodes is essential to achieve uniform deposition.

## Slide 56
Thank you for listening!

## Slide 57
//Lägg in fler plots här efter på större charge och andra figurer som Isak kanske kommenterar

## Slide 58: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-29