## Slide 1: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-29

## Slide 2: PLAN: 25 minute presentation
Introduction:
  Importance of batteries, improvements LMB>LIB (fig.), problems non-uniform growth (fig + in-depth), purpose of this thesis
Theory:
  Homogenous nucleation theory; main results (fig.), how does eta impact r and N (fig.)?
Methods:
  Cell assemblies (note importances; wave spring, no pressure); cycling protocol (fig.)
Results:
  passivation of Cu; J-dep.; pressure (C-cell and T-cell, r & angle dep. and morphology)
Conclusion: 2 min
  Passivation, J-dep. and pressure to achieve uniform deposition in LMBs
(Opposition and Questions from audience)

## Slide 3: Introduction
Batteries
Lithium-ion battery very common type; you probably have it!
Lighter and smaller by replacing graphite in LIB with Li-metal

## Slide 4: Batteries!
Opening: How many here have either a smartphone, a laptop, or a smartwatch?
Cool, then you are already fans of batteries, and you likely own at least one lithium-ion battery – a very common battery type
Say, would you like your device to be smaller, lighter, and have a longer battery life? Of course you would!
It’s easy, look: replace this graphite with Li and the cell increases its energy per weight and doubles the energy per volume – very nice!
Let’s use this battery. Oh… what’s happening? Without the graphite, Li gets deposited on the surface. The Li grows unevenly, and oh no – look – it reached the other side of the cell! It’s a short-circuit, and [thermal runaway] *BOOM* [cell explosion]
Yikes. Not good. Uneven deposition seems to be a problem.
There are in fact several problems.

## Slide 5: Batteries!
//LIB one of the most used batteries today
Looks like this.
If replace graphite with Li, increase specific energy and double the energy density
Would benefit e.g. electrical vehicles (extra range)
However, problems bcs. Li depos on surface! (n.s.)
600 Wh L–1 to 1200 Wh L–1
250 Wh kg–1 to 440 Wh kg–1

## Slide 6: Non-uniform deposition problems

## Slide 7: Non-uniform deposition problems

## Slide 8: Purpose of this thesis
Investigate pressure, current, passivation

## Slide 9: Deposition in a Li/Cu cell

## Slide 10: Deposition in a Li/Cu cell

## Slide 11: Deposition in a Li/Cu cell

## Slide 12: Deposition in a Li/Cu cell

## Slide 13: Deposition in a Li/Cu cell

## Slide 14: Deposition in a Li/Cu cell

## Slide 15: Deposition in a Li/Cu cell

## Slide 16: Nucleation
Notes: Li-ions in solution (liquid)  Li-metal (solid)

## Slide 17: Nucleation

## Slide 18: Nucleation

## Slide 19: Nucleation

## Slide 20: Nucleation

## Slide 21: Nucleation

## Slide 22: Nucleation

## Slide 23: Nucleation theory

## Slide 24: Nucleation theory

## Slide 25: Nucleation theory

## Slide 26: Nucleation theory

## Slide 27: Nucleation theory

## Slide 28: Nucleation theory

## Slide 29: Nucleation theory

## Slide 30: Nucleation theory

## Slide 31: Nucleation theory

## Slide 32: Nucleation theory

## Slide 33: Nucleation theory

## Slide 34: Specific scientific questions
The shape of the deposition curve
  Degree of passivation of the Cu surface
  Deposition current
Size and distribution of the nuclei
  Pressure between the Li and Cu
Notes: For different pressure, we need two different cell setups

## Slide 35: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 36: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 37: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 38: The C-cell
Cap
Spring
Spacer
Li
Separator
Cu
Gasket
Can

## Slide 39: The I-cell
Spring
Spacer
Nut
Sealing
rings
Metal rod
Main body
Li
Separator
Cu

## Slide 40: The T-cell
Nut
Metal rod
Sealing rings
Main body
Spacer
Li
Cu

## Slide 41: The T-cell

## Slide 42: The T-cell

## Slide 43: Deposition protocol

## Slide 44: Deposition protocol

## Slide 45: Deposition protocol

## Slide 46: Deposition protocol: σ

## Slide 47: Passivation of the Cu surface
Notes: T-cell, Jdeposition = 1 mAh/cm2
Time increase for lower sigma: 2 min for 0.50, 2 hour for 0.05, over 25 hours for 0.01

## Slide 48: Passivation of the Cu surface
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 49: Passivation of the Cu surface larger charge passed
Notes: T-cell, 1 mAh/cm2
sigma=1.00: no obvious nucleation; side reactions large enough to drive current without need for nucleation
Decreasing sigma  clearer deposition peak at higher overpotential
Larger overpotential  smaller nuclei, larger N  many sites for continued growth, lowering the necessity for further nucleation. Other words: more instantaneous nucleation (all nuclei form at the start and then they only grow).
Opposed to progressive nucleation, where nuclei continue to form as other grow

## Slide 50: Deposition current

## Slide 51: Deposition current with more passivation

## Slide 52: Deposition current with more passivation larger charge passed

## Slide 53: Pressure effects

## Slide 54: Pressure effects

## Slide 55: Pressure effects

## Slide 56: Pressure effects

## Slide 57: Pressure effects

## Slide 58: Pressure effects
2r = 1 µm
2r = 2 µm to 3 µm
2r ≥ 4 µm

## Slide 59: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 60: Pressure effects
N = 0.024 nuclei/µm2
2r = 1 µm
N = 0.022 nuclei/µm2
2r = 2 µm to 3 µm
N = 0.016 nuclei/µm2
2r ≥ 4 µm

## Slide 61: Pressure effects

## Slide 62: Pressure effects

## Slide 63: Pressure effects

## Slide 64: Pressure effects

## Slide 65: Pressure effects

## Slide 66: Pressure effects

## Slide 67: Pressure effects

## Slide 68: Pressure effects

## Slide 69: Conclusions
More instantaneous or more progressive nucleation depends on the current ratio of the side reactions and the deposition (σ).
The nuclei distribution (r and N) is influenced by the degree of passivation since that changes the nucleation peak (η).
Uniform pressure between the electrodes is essential to achieve uniform deposition.

## Slide 70
Thank you for listening!

## Slide 71
//Lägg in fler plots här efter på större charge och andra figurer som Isak kanske kommenterar

## Slide 72: Electrochemical deposition of lithium on copper
Gottfrid Olsson
2024-05-29