## Slide 1: 2024-03-13: SEM-06, reproducibility test
Gottfrid Olsson
Samples: V, X, Y, Z

## Slide 3: Sample X

## Slide 4: At edge

## Slide 5: Start seeing depositoin

## Slide 6: Start of deposition, different contrast/brightness/SEDMultiplierV

## Slide 9: About 1 mm downwards

## Slide 10: Different places, different magnifications

## Slide 14: Stor skrap? Might be from pushing down the Cu on the Cu tejp using the pincer

## Slide 15: Further down

## Slide 16: Even further down

## Slide 17: Still further down

## Slide 18: Yet further down

## Slide 20: Auger test

## Slide 21: Point 1 and 2

## Slide 22: Point 3 and 4

## Slide 23: Same place after looking at it for many minutes

## Slide 25: More deposition in crack/crevasse?

## Slide 27: Auger on bare Cu (close to edge of sample)

## Slide 28: Point 1 and 2 (bare Cu, no Li)

## Slide 30: Sample V (same build and cycling as sample X and Y)

## Slide 31: Edge, scratches

## Slide 32: Deposition, closer to middle than edge

## Slide 34: Another place; directional Li-deposition? Might be form the surface morphology from grinding?

## Slide 35: Another another place

## Slide 36: Directional in another direction

## Slide 38: Directional: meeting Li deposition at different angles: probably from grinding

## Slide 39: More directional

## Slide 41: Sample Y

## Slide 42: Different morphology

## Slide 43: Looks like worms/caterpillars

## Slide 44: But… further in we see more of the same deposition as in the other samples

## Slide 49: Sample Z (less deposition than the others)

## Slide 50: At edge

## Slide 51: At top edge: no deposition

## Slide 52: 1mm down (toward middle): light parts are edge of the grinding lines? Note: dark spots

## Slide 53: 2mm down: very few particles of Li

## Slide 54: 3mm down

## Slide 55: In the middle

## Slide 57: Some deposition

## Slide 58: Same place as before, small white particles

## Slide 59: Wait! Maybe the light parts ARE Li after all one pic with grinding lines, very little white (N.P.)…

## Slide 60: Moving just a little, we see white stuff in grinding lines (Li deposition)

## Slide 62: VERY small Li nuclei?