## Slide 1: 2024-03-08, SEM-05, washing times
Gottfrid Olsson, samples Q, R, S, T, U

## Slide 2: Testbilder 10kV1nA

## Slide 3: Sample Q: electrolyte on surface, no wash

## Slide 4: Black hole? Saw bubbles! Electrolyte/DME

## Slide 5: Edge of where electrolyte was applied /- black space is probably DME then

## Slide 6: Edge of sample, areas of both electrolyte and clean Cu

## Slide 7
Must clean in someway, otherwise cannot see anything!

## Slide 8: Sample R: electrolyte on surface, 1 min wash submerged in fresh DME

## Slide 9: Close to cut edge (middle), dark spots and bubbles?

## Slide 10: If zoom in, lots of bubbles (same place, different times) – still DME from washing on surface?

## Slide 11: Changed to 10kV5nA

## Slide 12
Hrrm, looks bad even though it was submerged in DME for 1 minute

## Slide 13: Sample S: Li-deposition, submerged in DME for 10 seconds

## Slide 14: Edge of sample

## Slide 15: Further in towards centre: salt/DME (bubbles)

## Slide 16: Even if there is Li deposition, everything is covered in shite

## Slide 17: Close to edge, bare Cu

## Slide 18: Dead Li? (further zoom in on previous image):changed brightness and contrast for these two

## Slide 19: Something’s happening when you look at a place for long

## Slide 20
Something’s happening when you look at a place for long

## Slide 21
A lot of shite, seems like 10 seconds wash (submerged in DME) is not enough

## Slide 22: Sample T: Li-deposition, submerged in DME for 1 minute
10kV10nA

## Slide 23: Close to edge

## Slide 24: Granslandet mellan kant (right) och mitten, deponering (left)

## Slide 25: Li-deposition

## Slide 26: Center

## Slide 27: Center, different place

## Slide 29
Li deposition, no shite (or very little)
 1 minute might be enough washing
BUT! Still dark spots in the background – eaten Li from washing in DME?

## Slide 30: Sample U: Li-deposition, submerged in DME for 5 minutes (Li might have delaminated from metal plunger during assembly, so bad or irregular Li-deposition should not be surprising)

## Slide 31: At edge

## Slide 32: At edge, more zoom (need better focusing…)

## Slide 33: 1mm from edge

## Slide 34: 2-3mm in

## Slide 35: Close to center 4-5 mm from edge

## Slide 36: Further down, even further down (looks the same)

## Slide 38
Looks very much more homogenous Li deposition (even though it might be very much to little)
No shite everywhere! – longer washing time better(?), at least longer than 10 seconds