## Slide 1: Gottfrid sample A (center ?)

## Slide 2: Edge of deposition

## Slide 3: Actual edge of Cu sample, no Li (?)

## Slide 4
Saw black parts with spots
Started bubbling after taking picture (see below)
Josef thinks it might have been salt

## Slide 8: Edge of deposition, more sparse Li

## Slide 9: Close by, more dense Li

## Slide 10: Closer to edge of sample, Li?

## Slide 11: At edge, no nucleated Li

## Slide 12: Edge of Li deposition, more spaghetti-like

## Slide 13: Edge of Li deposition

## Slide 14: Edge of Li deposition

## Slide 15: Starting from this edge, moving inwards (arrow)

## Slide 16: About 1mm in from edge of deposition

## Slide 17: About 2mm in from edge of deposition

## Slide 18: About 3mm in from edge of deposition

## Slide 19: About 4mm in from edge of deposition

## Slide 21: Sample B, edge of something (not Li)

## Slide 23: Edge of deposition?

## Slide 24: Edge of deposition (EoD)

## Slide 25: EoD

## Slide 26: EoD

## Slide 27: 0.3 mm in from the EoD in previous slide

## Slide 28: EoD

## Slide 29: 0.3 mm from EOD

## Slide 30: EoD

## Slide 31: EoD (?)

## Slide 32: EoD

## Slide 33: EoD

## Slide 34: EoD

## Slide 35: 1 mm towards center from EoD

## Slide 36: 2mm towards center from EoD

## Slide 37: 3mm towards center from EoD

## Slide 38: 4 mm towards center from EoD

## Slide 40: Sample D, center

## Slide 41: Sample D, center

## Slide 43: Sample C, edge

## Slide 44: Sample C, EoD or outside
Lots of bubbles formed in this region

## Slide 45: Further towards center, EoD?

## Slide 46: EoD

## Slide 47: Further towards egdge *from last position

## Slide 48: EoD

## Slide 49: EoD

## Slide 50: Beam damage to Li
Pictures taken a few seconds apart at high mag

## Slide 51: 1 mm towards center from EoD

## Slide 52: 2mm towards center from EoD

## Slide 53: 3 mm towards center from EoD

## Slide 54: 4mm towards center from EoD