## Slide 1: 2024-02-21
SEM-03
Deposition amount
Samples I, J, and K
(sample L did not go well, no visible Li deposition)

## Slide 2: Sample I (0.005 mAh cm-2)

## Slide 3: Polished Cu (no Li) close to edge

## Slide 4: Closer to middle, probably salt/skrap

## Slide 5: Closer to middle, might be Li (very small, very sparse)

## Slide 6: No signs of blatant Li deposition on sample I

## Slide 7: Sample J (0.01 mAh cm-2)

## Slide 8: 2mm from edge

## Slide 9: Edge of deposition (EOD)

## Slide 10: Middle of the band (annulus) of deposition

## Slide 11: Closer to middle (band of deposition to the left now)

## Slide 12: Eye of the storm, middle of annulus

## Slide 13: Right part of annulus deposition

## Slide 14: Lower right part of annulus

## Slide 15: Lower part of annulus, different magnifications (test ImageJ analysis)

## Slide 16: Lower part of annulus, different magnifications (test ImageJ analysis)

## Slide 17: Lower part of annulus, different magnifications (test ImageJ analysis)

## Slide 19: Sample J:
clear Li deposition
nuclei approx. 1 micrometer in diameter
Deposition region is an annulus following the circumference of the 5 mm Li disk used for deposition

## Slide 20: Sample K (0.025 mAh cm-2)

## Slide 21: 1mm from edge

## Slide 22: 2mm from edge

## Slide 23: EOD, approx. 2,5 mm from edge of sample

## Slide 25: Inner radius of EOD

## Slide 28: Eye of the storm, middle part, little Li

## Slide 30: Lower part of upper deposition band (note rings, ‘halo’s around dead? Li nuclei)

## Slide 32: Upper part of lower deposition band

## Slide 33: Middle part of lower deposition band

## Slide 34: Lower part of lower deposition band

## Slide 35: Lower edge of lower deposition band

## Slide 36: Below lower edge